Nickel Formate

Molecular formula：C2H2NiO4，molecular weight：148.72

Properties：This product is a shiny light green crystals, slightly soluble in water and oxalic acid, soluble in acid, soluble in alkali metal salt solution of oxalic acid and ammonia, the solubility careful heating to 130 ~ 140 ℃, lose crystal water, become anhydride. During 180 ~ 200 ℃ is decomposed into nickel, carbon monoxide, carbon dioxide, hydrogen, methane and water.Soluble in water, insoluble in formic acid.

Quality Standard：

| Index | Company standard |
| --- | --- |
| 镍 (Ni) % ≥ | 38 |
| 铁 (Fe)% ≤ | 0.006 |
| 铜 (Cu)% ≤ | 0.005 |
| 锌 (Zn)% ≤ | 0.003 |
| 铅 (Pb)% ≤ | 0.001 |
| 钴 (Co)% ≤ | 0.2 |

Areas of application: used in nickel plating, nickel powder and nickel catalyst.

Packing: 25 kg bags