WEI FANG QI HUI CHEMICALS CO., LIMITED

SOUTH OF GUANGCHANG STREET,EAST OF LUHAI ROAD,BINHAI

ECONOMIC DEVELOPMENT ZONE

TEL: +8618866701380    FAX: 0086-536-5336333

CERTIFICATE OF ANALYSIS

DATE: Sep.15TH, 2015

PRODUCT NAME: SODA ASH

PRODUCTION DATE: Sep, 10th, 2015

Soda ash light

ITEM                                       INDEX              RESULT

Content                                  99.2%min             99.62%

chlorides                                0.7%MAX             0.34%

Sulphate                                 0.03% max            0.015%

Fe                                         0.003%max           0.0007%

Water insoluble matter                 0.03%max            0.008%

lgnition loss）                            0.8%max             0.1%

Packing: packed in plastic woven bags of 40/1000kgs net each

SODA ASH DENSE

Item                          index                testing  result

Content                     99.2%min                     99.47%

chlorides                   0.7%max                      0.48%

Sulphate                    0.03%max                     0.03%

Fe                          0.004%max                   0.0009%

Water insoluble            0.04%max                    0.008%

lgnition loss                 0.8%max                     0.3%

bulk density                  0.9g/ml                    0.94g/ml

Packing: packed in plastic woven bags of 50/1000kgs net each