- Nickel Fluoride

Molecular Formula: NiF2·4H2O
Molecular Weight： 168.70
Properties： Green powder, has the water absorbability, soluble in water.

The main technical indicators: (in %)

| Content | % |
| --- | --- |
| (Ni)≥ | 31-32 |
| (F)≥ | 22.1 |
| (Cl)≤ | 0.05 |
| (SO4)≤ | 0.10 |
| (Cu)≤ | 0.01 |
| (Fe)≤ | 0.02 |
| (Zn)≤ | 0.05 |

Application: fluoride, aluminum alloy hole sealing agent.

Storage: moisture, sealing preservation.

Packing: packed in plastic woven bag, 25 kg per bag.