Product quality inspection report

| Product name: Hexagonal BN | Unit: |
| --- | --- |
| Quantity：100g | Quality Standards：QJ/YH02·08-89 |
| Report date： | Product batch： |
| The inspection items | Test results |
| Hexagonal BN （%） | ≥99 |
| Free boron oxide （%） | ≤0.2 |
| Sodium oxide（Na2O） （%） | ≤0.10 |
| Magnesium Oxide(MgO) （%） | ≤0.018 |
| Granular Size: um | According to the customer demand |
| Appearance：White powder |  |
| Inspectors: |  |
| Liaoning boron Technology Company Limited （YingKou PengDa Fine Chemicals Co. Ltd） |  |