溶剂红24

CAS：85-83-6

分子式：C24H20N4O

结构式：

国外相应品牌：Oleosol Red BB(NSK), Waxoline Red O(ICI)

特性：带蓝光透明大红色油溶性染料，具有较好的耐热性和耐光性，着色力高，色调鲜艳、明亮。

色调：蓝光红

用途：主要用于油脂、药水、肥皂、蜡烛、橡胶玩具、塑料制品、油墨和透明漆等的着色。

性质：密度0.33g/cm3，熔点180℃，耐光牢度（PS中）：5-6级，耐热性（PS中）：250 ℃

应用范围：

| PS | HIPS | ABS | PC | RPVC | PMMA | SAN | AS | PA6 | PET |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ★ | ○ | ○ | △ | ★ | ★ | ○ | △ | - | - |

注："★"优良、○适用、"△"不推荐。

在有机溶剂中的溶解能力：在20℃时染料在每升溶剂中溶解的克数。

| 丙 酮 | 乙酸丁酯 | 甲苯 | 二氯甲烷 | 乙醇 |
| --- | --- | --- | --- | --- |
| 20.2 | 21.7 | 37.3 | 32.8 | 21.1 |

注：以上数据仅供使用时参考，批量使用前，应对产品进行测试后方可实用。

Solvent Red 24
CAS：85-83-6

Molecular Formula：C24H20N4O

Structural Formula：

Structure: Sulphonazo series

Foreign corresponding Product: Oleosol Red BB(NSK), Waxoline Red O(ICI)

Properties: The product is bluish transparent scarlet oil solvent dye. It is of good heat resistance, good light fastness and strong coloring power.

Hue：Bluish red

Use: Mainly used in coloring of grease, liquid medicine,soap, wax, rubber toys, plastics, printing ink and transparent paint etc.

| PS | HIPS | ABS | PC | RPVC | PMMA | SAN | AS | PA6 | PET |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | - | - |

Note: ""Superior ,"¡ð"Applicable ,""Not Recommended.

Physical properties, light fastness and Recommended Dosage:

| Density(g/cm3) | Melting Point () | Light Fastness (In PS) | Recommended Dosage |  |
| --- | --- | --- | --- | --- |
|  |  |  | Transparent | Nontransparent |
| 0.33 | 180 | 5-6 | 0.025 | 0.05 |

Light Fastness: Consist of 1st to 8th grade, and the 8th grade is superior, the 1st grade is bad.

The thermal resistance in PS can reach to 250.
Degree of pigmentation: 0.05% dyes+0.1%titanium white powder R

Solubility in Organic Solvent:

| acetone | butyl acetate | methylbenzene | dichloromethane | ethylalcohol |
| --- | --- | --- | --- | --- |
| 20.2 | 21.7 | 37.3 | 32.8 | 21.1 |

The grammage dissolve in one litre solvent at 20.

NOTE: Above data is only for reference.